Natural fibre cross sectional area, its variability and effects on the determination of fibre properties.

J. L. Thomason, J. Carruthers.

University of Strathclyde, Department of Mechanical Engineering, 75 Montrose Street, Glasgow G1 1XJ, United Kingdom.

ABSTRACT

The results of a study on the measurement of fibre cross section and its variability in flax and sisal fibres are presented. Cross section values obtained from fibre “diameter” measurements were more than double the values obtained from actual observation of cross sections of the same individual fibres. The overall conclusion is that fibre “diameter” measurement is not an attractive method for accurate estimation of cross sectional area of these natural fibres. This conclusion is significant for researchers engaged in micromechanical investigation of natural fibre composites since differences in fibre cross section translate directly into differences of the same magnitude in the values obtained for the fibre modulus and strength. The error in fibre cross section introduced by the “diameter” method scales with the average fibre “diameter” which may also result in erroneous observations of fibre modulus and strength scaling inversely with natural fibre “diameter”. The difference in average cross section observed from fibre to fibre was significantly greater than the variation along the length of each individual fibre. The minimum to maximum cross section variability of individual flax fibres was found to be approximately twice that observed for sisal fibres.

INTRODUCTION

The use of glass fibre reinforced polymer materials has increased dramatically during the last half century, becoming the standards of high performance in automotive, aeronautical and innumerable other high performance applications. However, prior to the tremendous success and growth of the petrochemical industry in 20th century the majority of the materials used were obtained from renewable resources. So the use of renewable materials is not a new idea and in recent years there has been a growing renewal of interest in the research of fibres derived from natural sustainable sources as potential reinforcements for high performance composite materials. It has been claimed that natural fibres show significant potential as environmentally friendly alternatives to conventional reinforcements such as glass fibres [1-3] although these claims often ignore the well documented low levels of shear and transverse modulus of natural fibres [4-6]. Nevertheless, one of the basic underlying assumptions in virtually all micromechanical analysis and modelling of fibre reinforced composites is that the fibres are circular in cross section and that the fibre diameter is constant along the fibre length. Efficient determination of the simplest engineering parameters such as modulus and stress depends heavily on these assumptions. Furthermore, many researchers have identified the fibre-matrix interface in natural fibre composites as an area of potential weakness and consequently there has been a significant focus on the investigation of methods to tailor the level of natural fibre-polymer interactions [1-8]. This has naturally resulted in application of many of the fibre and interface characterisation tools, developed using man-made fibres, to natural fibre technology. These include many single fibre methods for interface characterisation [7-9] and determination of single fibre strength distributions [8,10-13]. These methods present researchers with significant technical and resource challenges, however up to now measurement of fibre cross section and its uniformity has not been high on the list of those challenges.

Many types of natural fibre have been identified which appear to have some appropriate mechanical properties for structural purposes, being of low density or high specific strength and stiffness. Sisal and flax are examples of such fibres. Unfortunately these cellulose based fibres suffer from the natural variability which is inherent in materials sourced directly from nature. Consequently the documentation of their structural properties usually does not quote specific values but rather present ranges which are often of the same order of magnitude as the average values themselves [1-3]. This presents engineers, used to the availability of consistent and accurate mechanical property data of manmade fibres, with a significant challenge in terms of designing reliable structures based on these natural fibre composites. Despite the inherent natural variability of these fibres it is possible that a significant contributor to the large range of specific properties found in the literature may be the cross-sectional shape of natural fibres. The measurement of the longitudinal mechanical properties of traditional reinforcement fibres depends on their cross-section being circular and uniform along their length. This allows a simple measurement of fibre diameter to be used to calculate the fibre cross-section area (CSA) required to obtain modulus and strength from an experimental load-displacement curve. Most natural fibres are neither circular in cross section nor uniform along their length. Consequently, a simple “diameter” measurement of a transversely viewed fibre image may not be sufficient to accurately assess cross-section at any point and may certainly not be representative of the fibre at any other point. In this paper we present the results of an investigation of the determination of the CSA of single fibres of flax and sisal.

EXPERIMENTAL

Flax fibres (grown in Germany) and sisal fibres (grown in Brazil) used in this study were sourced from Wigglesworth fibres[13]. Single technical fibres were meticulously separated from large flax and sisal yarns of intertwined fibres. The fibres were separated from one another until no fraying could be seen with the naked eye. To investigate the diameter method of CSA measurement, fibres were photographed at four separate positions while under transverse observation using a Nikon Epiphot inverted microscope (at 50x magnification). This allowed an average fibre “diameter to be estimated, under the assumption of uniformly circular cross section fibres. To directly examine the CSA along the fibre length, these same individual fibres were glued to card and then embedded vertically in resin blocks. These embedded samples were prepared for microscopy by grinding them down to a fine finish using progressively finer grinding papers (120, 1200, 2400 and 4000 grade). The fibre cross sections were then photographed under the microscope at 100x magnification. Samples were then repeatedly ground, polished and photographed, in roughly 2 mm steps, following the above procedure, to give ten CSA measurement along a 20 mm length of fibre. Each fibre micrograph was traced using Image Pro Plus analysis software to find the CSA.

RESULTS AND DISCUSSION

Figure 1 shows some typical cross section images obtained on sisal and flax fibres using optical microscopy. The non-circular cross section of these natural fibres is clearly illustrated in the micrographs in this Figure. The outline of the fibres has been traced and highlighted and it is this outline which was utilised in the image analysis software to evaluate the fibre CSA. Figure 1 highlights the complex internal structural of these natural fibres. These ‘technical’ fibres are actually composite structures consisting of an assembly of many elementary fibres which have a polygonal cross section, allowing them to fit closely together. Figure 2 shows the results of the measurement CSA of twelve individual sisal fibres at ten positions along a 21 mm length of each fibre. It can be observed that there is quite some variation in CSA along the length of some fibres whereas other fibres appear relatively uniform. What is also clear from the results in Figure 2 is that the difference in CSA observed from fibre to fibre is significantly greater than the variation along the length of each individual fibre. Similar trends in the variability of flax fibre CSA can be seen in Figure 3. The flax fibres exhibit a significantly lower average CSA compared to the sisal fibres. Nevertheless, it is clear from Figure 3 that the inter-fibre CSA variability for flax is also greater that the intra-fibre variability. A further analysis of the data presented in Figures 2 and 3 is shown in Table 1. The data presented in this Table show the standard deviations of the various fibre CSA averages calculated as a percentage of the relevant average. The values in Table 1 confirm the observations stated above that the inter-fibre CSA variability is significantly greater than the intra-fibre CSA variability for both sisal and flax fibres. Moreover, it appears from the data presented in Table 1 that the flax fibres show greater levels of both types of CSA variability compared to the sisal fibres. This is an interesting correlation with the larger spread in modulus values observed in the literature on flax fibres. Furthermore, the fibre to fibre variability appears to be much greater than the variability along (relatively short) lengths of individual fibres. It can also be concluded from this data that the use of an average CSA obtained over a range of individual fibres could lead to significant errors in the calculation of fibre mechanical performance from load-displacement data and that the use of (even single) measurements of the CSA of each individual fibre will probably result in a more accurate estimation of the properties of natural fibres.

Table 1 Analysis of sisal fibres cross section variations

|  | Average CSA (mm2) | % standard deviation of the average CSA |
| --- | --- | --- |
|  |  | Intra-fibre | Inter-fibre |
| Sisal | 0.0272 | 7.3% | 30.3% |
| Flax | 0.0125 | 9.2% | 42.0% |

Figure 4 compares the value obtained for the fibre CSA obtained by two different methods for each individual fibre. The first value is calculated, assuming a circular fibre cross section, from an average fibre “diameter” obtained from four measurements of fibre diameter taken along individual fibre gauge lengths observed at right angles to the main fibre axis. This is a method commonly employed in many papers reporting investigations on natural fibres and their composites [7-14]. These values are plotted against the average of four CSA observations on each of the same individual fibres after testing, embedding, sectioning and polishing. As is common with natural fibres there is considerable scatter observed in the data presented in Figure 4. However, notwithstanding the degree of scatter it is striking that the CSA values obtained from fibre “diameter” measurements are on average double or more the values obtained from actual observation of the fibre cross sections. Despite the scatter observed in Figure 4, analysis of the data indicates that the averages for the two fibres fall outside the 95% confidence limits of the other fibre. Consequently, we can state that flax fibres show a statistically significant greater potential error in using fibre “diameter” calculated CSA. However, the overall conclusion is that fibre “diameter” measurement is not an attractive method for accurate estimation of CSA of either of these natural fibres. This observation has important consequences for those researchers engaged in the determination of the properties of natural fibres. The above results indicate that use of a “diameter” determined fibre CSA may lead to the underestimation of properties such as modulus and strength by up to 60%. This is in good agreement with very recent results from a study of jute fibre diameter by Virk [15] who suggested the use of a “fibre area correction factor” of 1.42 in the measurement of fibre modulus and strength to account for the overestimation of the fibre CSA by the diameter method. Figure 5 shows the results for the ratio of the “diameter” calculated to measured fibre CSA plotted against the fibre “diameter”. It can be seen for most of these flax and sisal fibres a much greater correction factor would be necessary in order to obtain a reasonably accurate estimation of the fibre mechanical properties from single fibre testing. Moreover, it is clear from Figure 5 that there is a strong correlation between the required “correction” and the apparent fibre diameter. It also appears that the error from using a “diameter” calculated fibre CSA is greater for flax fibres compared to sisal fibres. The higher slope of the flax data may be indicative of a higher average aspect ratio for the flax fibre cross section.

One potentially significant result of the error in CSA obtained using the “diameter” method is shown in Figure 6. These data show the apparent dependence of the Young’s modulus of these fibres which would be obtained assuming a diameter independent value (flax = 71 GPa, sisal = 30 GPa) but including the diameter dependent error in CSA observed in Figure 5. It can be seen that the “diameter” effect on the error in estimating the fibre CSA can lead to a situation where the fibre modulus appears to be inversely correlated with “diameter”. A number of papers have presented results indicating such an effect [11,12,14].  Of course it is possible that the modulus of natural fibres is indeed inversely dependent on the apparent fibre “diameter”. However, Figure 6 indicates that there is also significant room for an artificial dependence to be observed if the “diameter” method is employed to estimate single fibre CSA. It is relatively easy to qualitatively understand this effect when considering the transverse observation of a non-circular cross section cylinder to obtain a “diameter” measurement. Figure 7 shows the outline of the flax and sisal fibres pictured in Figure 1 compared to a possible circle and ellipse. It is clear from this Figure that an ellipse is a much better model of a natural fibre cross section than a circle. It is also well known that natural fibres exhibit a level of twist along their length which means that the apparent diameter of a fibre with a constant elliptical cross section fibre will vary along its length. As illustrated in Figure 8 an ellipse centred on the origin can be expressed as the path of point X(t),Y(t) where

X(t) = ½ACos(t)Cos() - ½BSin(t)Sin()			  	(1)

Y(t) = ½ACos(t)Sin() + ½BSin(t)Cos()				 (2)

as the parameter t varies from 0 to 2π. Here A and B are the ellipse's major and minor axes respectively and is the angle between the X-axis and the major axis of the ellipse. The experimental measurement of a natural fibre “diameter” (D) is the equivalent of measuring the width of the projection of the ellipse in Figure 8 on the x-axis which is equal to 2Xmax, where Xmax is the maximum value of X for any angle .

dX/dt = -½ASin(t)Cos() - ½BCos(t)Sin() =0, hence Tan(tmax) = -(B/A)Tan()	 (3)

The value of Xmax can be obtained as shown by setting the differential of equation 1 equal to zero and solving for tmax and then substituting tmax into equation 1 to obtain Xmax at any angle . Finally an average value for Xmax , which is equivalent to the average value of fibre “diameter” measured at many points along the fibre length, can be obtained over the range 0<<90. This average value (D) of apparent ellipse diameter should approach the average value of the equivalent natural fibre diameter if sufficient fibre diameter measurements are made along a length of fibre covering one natural twist in the fibre. Figure 9 presents the results from this simple analysis comparing the ratio of D2/AB over the range 0<<90 for ellipses with aspect ratios between 1 (a circle) and 5. The D2/AB ratio is the equivalent to the y-axis of Figure 5 the ratio of fibre CSA obtained by the “diameter” method to the actual fibre CSA. It can be seen in Figure 9 that this ratio depends strongly on both observation angle and on the aspect ratio of the elliptical cross section. Although the ratio is slightly less than unity at high angles it is significantly greater than unity for over the majority of the Figure. Consequently the average value of the D2/AB ratio over the full range of angles is always greater than unity and increases strongly with increasing ellipse aspect ratio (maintaining constant area) as shown in Figure 10.

Figure 11 shows the experimental data from Figure 5 for the “diameter”/actual CSA ratio of flax and sisal compared with the results from the simple model presented above. The lines show data calculated for the average D2/AB ratio for ellipses with varying aspect ratio and constant values of CSA. The six lines represent minimum, maximum, and average values of CSA for the two fibre types. It can be seen that the model lines form envelopes which contain all the experimental data and the lines for the average fibre CSA form a reasonable representation of the trends of the experimental data. Clearly the spread in the data could well be explained by the fibre to fibre variability of the CSA and the fact that the fibres do not have an exactly elliptical cross section. These results would appear to strongly indicate that natural fibre CSA cannot be well estimated by an assumption of circularity and the use of simple “diameter” measurements. The above results indicate some of the challenges of characterising natural fibres, such as flax and sisal, where many of the micro-structural parameters required for dependable design of fibre reinforced composite exhibit high levels of variability. Single fibre analysis of traditional man-made reinforcements is already highly resource intensive. Nevertheless, it appears from the results presented here that the time saving strategy of assuming natural fibres have a constant circular cross section and using a “diameter” measurement to characterise cross sectional area can introduce high levels of error into the determination of fibre modulus and strength.

CONCLUSIONS

The ability to efficiently and accurately characterise the cross sectional area of reinforcement fibres is critical to the development of a database of engineering performance of reinforcement fibres. A commonly employed shortcut in this area is the assumption that fibre cross section is uniformly circular, which reduces CSA determination to a simple measurement of fibre diameter. The results of this study on the measurement of the CSA of flax and sisal fibres revealed significant variation in fibre CSA along the length of many fibres whereas other fibres appear relatively uniform. However, the difference in average CSA observed from fibre to fibre was significantly greater than the variation along the length of each individual fibre. Furthermore, CSA values obtained from fibre “diameter” measurements on these flax and sisal fibres were found on average to be more than double the values obtained from direct observation of the fibre cross sections. Such differences in CSA translate directly into differences of the same order of magnitude in the determined values of fibre modulus and strength. Consequently, the overall conclusion is that fibre “diameter” measurement is not a particularly attractive method for accurate estimation of CSA for these natural fibres. The level of error in the fibre CSA introduced by the “diameter” method appears to scale with the average fibre “diameter” which may go some way to explaining published observations of fibre modulus and strength scaling inversely with natural fibre “diameter”.

REFERENCES

- Bledzki, A.K. and Gassan, J., Composites Reinforced with Cellulose Based Fibres, Prog Polym Sci. 1999;24:221-274.

- Goda, K. and Cao, Y., Research and development of fully green composites reinforced with natural fibers, J Sol Mech Mater Eng 2007;1(9):1073-1084.

- Hughes, M., Carpenter, J. and Hill, C., Deformation and fracture behaviour of flax fibre reinforced polymer composites, J Mater Sci 2007;42:2499–2511

- Thomason, J.L., Dependence of interfacial strength on the anisotropic fiber properties of jute reinforced composites, Polym Compos 2010;31:1525–1534.

- Thomason, J.L., Why are Natural Fibres failing to deliver on Composite Performance? proceedings 17th Int Conf Composite Materials, July 2009.

- Cichocki, F.R. and Thomason, J.L., Thermoelastic anisotropy of a natural fiber, Compos Sci Technol 2002;62:669–678.

- Li, Y., Pickering, K.L. and Farrell, R.L., Determination of interfacial strength of hemp reinforced polypropylene,  Compos Sci Tech 2009;69:1165–1171.

- Park, J.M., Quang, S.T., Hwang, B.S. and DeVries, K.L., Interfacial evaluation of modified Jute and Hemp/polypropylene composites using micromechanical technique and acoustic emission, Compos Sci Technol 2006;66:2686-2699.

- Beckermann, G.W. and Pickering, K.L., Engineering and evaluation of hemp fibre reinforced polypropylene composites, Compos Part A: 2009;40:210-217.

- Xia, Z.P., Yu, J.Y., Cheng, L.D., Liu, L.F. and Wang, W.M., Study on the strength of jute fibres using modified Weibull distribution, Compos Pt A 2009;40:54-59.

- Baley, C., Analysis of the flax fibres tensile behaviour and analysis of the tensile stiffness increase, Compos Part A 2002;33:939-948.

- Lamy, B. and Baley, C., Stiffness prediction of flax fibers-epoxy composite materials, J Mater Sci Letts 2000;19:979-980.

- Symington, M.C., Banks, W.M., West, O.D. and Pethrick, R.A., Tensile Testing of Natural Fibers, J Compos Mater 2009;43(9):1083-1108.

- Virk, A.S., Hall, W. and Summerscales, J., Failure strain as the key design criterion for natural fibre composites, Compos Sci Technol 2010;70:995–999

- Virk, A.S., Numerical models for natural fibre composites with stochastic properties, PhD thesis, University of Plymouth 2010.

- Bunsell, A., in Fibre Reinforcements for Composite Materials, Composite Materials Series 2, Elsevier Amsterdam 1988.

- Qiu, Y., Batchelor, S.D., Jack, P.R., McCord, M.G., Estimation of the modulus of a fiber with variable radius, Compos Sci Technol 2000;60(14):2731-2737.

- Weibull, W. J., A statistical distribution function of wide applicability, J Appl Mech, 1951;18:293-297

Figure 1. Cross section of single Flax and Sisal fibre

Figure 2. Cross section variations along sisal fibres

Figure 3. Cross section variations along flax fibres

Figure 4. Fibre cross sectional area – directly measured versus diameter calculated

Figure 5. Diameter dependence of ratio of diameter calculated to measured fibre CSA

Figure 6. Apparent fibre modulus diameter dependence caused by CSA “diameter” method systematic error

Figure 7. Fibre cross section model – circle versus ellipse

Figure 8. Cross section variations along flax fibres

Figure 9. CSA ratio versus orientation and aspect ratio of ellipse

Figure 10. Average CSA ratio versus aspect ratio of ellipse

Figure 11. Comparison of CSA ratio from experiment and from ellipse model